Acrylic

0.375

8mm at 60 watts

Will cut but not consistently across the area of the bed, should use a lower speed.

7mm at 60 watts

So far the best value, consistently cutting across the entire bed area.

0.236

0.177

Plywood

.250

40mm at 60 watts